## Slide 1
On 3D printing PPF for bone tissue engineering.

## Slide 6
oxybenzone
Over 33% needed as opposed to 3%-4% TiO2 to achieve same layer thickness.
Layer-thickness (z-resolution)
z

## Slide 8
SUNSCREEN
SPF

## Slide 12
Increase in Resolution
Just TiO2
TiO2 and Oxybenzone
No open pores
All open pores

## Slide 13
TiO2 alone
“dark cure”

## Slide 14
TiO2 alone
TiO2 + Oxybenzone
“dark cure”
No “dark cure”

## Slide 15
1:1 PPF:DEF
1% Irgacure 819
1% TiO2
28% Oxybenzone
The Magic Potion
With respect to mass of PPF & DEF
PPF Parameters:
Mn: 866 da
PDI: 1.3

## Slide 22
Time Out!!
Potential Fixes:
Increase the light intensity
Tighten up the bandwidth

## Slide 23
The Perfactory Microbeta
Lamp warm up time:
Calibration required:
Calibration time:
User control of build-style:
Control of Job-file:
Resin required:
GUI via computer:
Micro
P3
0 min
None
0 min
Full
Full
40 ml
Yes
30 min
Yes
Up to 2 hours
Very limited
Limited
200 ml
No
Key Benefits:
80% less material required to run it!

## Slide 27
1% Irgacure 819
2% Irgacure 819
3% Irgacure 819
“The Goldilocks zone.”
You are here

## Slide 28
Material Variables:
Polymer kind
Polymer concentration
Polymer molecular weight [da]
Polymer polydispersity [unit-less]
Diluent/Solvent kind
Diluent/Solvent concentration
Photoinitiator kinds
Photoinitiator concentrations
Dyes (kinds and concentrations)
Pigments (kinds and concentrations)
Origin date
Printer Variables:
Light intensity [mW/dm2]
Light wavelengths [nm]
Burn-in range [μm]
Burn-in range exposure time [s]
Standard range [μm]
Standard range exposure time [s]
z-step size [μm]
Base plate height [μm]
Peel velocity [μm/s]
Separation velocity [μm/s]
Residence time before exposure [s]
Residence time after exposure [s]
Basement type [material]
Post Processing Variables:
Post cure time
Wash method

## Slide 29
Material Variables:
Polymer kind
Polymer concentration
Polymer molecular weight [da]
Polymer polydispersity [unit-less]
Diluent/Solvent kind
Diluent/Solvent concentration
Photoinitiator kinds
Photoinitiator concentrations
Dyes (kinds and concentrations)
Pigments (kinds and concentrations)
Origin date
Printer Variables:
Light intensity [mW/dm2]
Light wavelengths [nm]
Burn-in range [μm]
Burn-in range exposure time [s]
Standard range [μm]
Standard range exposure time [s]
z-step size [μm]
Base plate height [μm]
Peel velocity [μm/s]
Separation velocity [μm/s]
Residence time before exposure [s]
Residence time after exposure [s]
Basement type [material]
Post Processing Variables:
Post cure time
Wash method

## Slide 31
Camphorquinone

## Slide 32
Camphorquinone
Result: A polymer puddle

## Slide 33
Irgacure 784
Zhang. Et al. (2011). Development of Photocrosslinkable Urethane-Doped Polyester Elastomers for Soft Tissue Engineering
Ciba Specialty Chemicals Inc. Edition: 2.4.98, Basle
A NEW HOPE
Biocompatible1
Favorable absorption profile2

## Slide 34
Irgacure 784
Result: A polymer puddle

## Slide 35
6 mm x 12 mm Solid Cylinder (1.5:1 PPF:DEF, 3% BAPO, 3% 784)
Build Parameters:
Printer: Micro
Intensity: 267 mW/dm2
Exposure time: 120 s
z-step: 50 μm

## Slide 36
Chart: 6 mm x 12 mm Solid Cylinder (1.5:1 PPF:DEF, 3% BAPO, 3% 784)
 | -0.58167 | -0.95288 | -1.3743 | -1.7992 | -2.2812 | -2.8153 | -3.3295 | -3.9652 | -4.5598 | -5.1541 | -5.8736 | -6.4719 | -7.0913 | -7.8154 | -8.4644 | -9.1773 | -9.9177 | -10.6322 | -11.2809 | -12.0005 | -12.7339 | -13.4123 | -14.1685 | -14.9044 | -15.5555 | -16.2579 | -16.9868 | -17.6356 | -18.3648 | -19.0853 | -19.7378 | -20.4326 | -21.0318 | -21.7696 | -22.3654 | -22.9348 | -23.5451 | -24.0892 | -24.6686 | -25.2722 | -25.7621 | -26.2882 | -26.7364 | -27.2831 | -27.6821
Almost 1.0 GPa!!
Previous studies showed maximum PPF modulus as: 195.3 +/- 17.5 MPa.

## Slide 37
Chart: 6 mm x 12 mm Solid Cylinder (1.5:1 PPF:DEF, 3% BAPO, 3% 784) to failure
Avg. Modulus: 334 MPa

## Slide 40
Hypothesis:
Adhesion to the basement is a serious factor.
Shear forces due to PSA basement during build may be resulting in failure at extended time points.
What we know about adhesion:
Grillet et al. (2012). Polymer Gel Rheology and Adhesion.

## Slide 41
The answer!
Return of the Perfactory
Benefits:
Higher intensity than Micro
Peel mechanism
PSA not required

## Slide 42
The build
Resin:
Name: BY
1:1 PPF:DEF
Mn: 933 da
Polydispersity: 1.9
3% Irgacure 819
0.5% Irgacure 784
Build parameters:
Printer: Perfactory P3
Intensity: 350 mW/dm2
Exposure time: 30 s
Slow peel

## Slide 44
Compression Test Parameters:
Instron
Load Cell: 100 lbf (444 N)
Strain Rate: 0.1 mm/s
Max Strain: 2 mm
~ 6 mm
~ 2.75 mm
Nominal Part parameters:
Height: 6 mm
Outer diameter: 2.75 mm
Wall thickness: 125 μm
Pore size: 350 μm
Compression Testing

## Slide 45
Chart: Green vs. Post-Cured

## Slide 46
Chart: Elastic Modulus
Green | 13.09
Post Cured | 282.635
Error bars: +/- 1 std. dev
Resin:
1:1 PPF:DEF
3% Irgacure 819
0.5% Irgacure 784
Post Cure Time: 480 min
Result:
1800% increase in modulus with post-curing.

## Slide 47
Chart: Max Compressive Strength
Green | 0.44793
Post-Cured | 10.3092
Error bars: +/- 1 std. dev
Resin:
1:1 PPF:DEF
3% Irgacure 819
0.5% Irgacure 784
Post Cure Time: 480 min
Result:
2200% increase in compressive strength with post-curing.

## Slide 48
1:1 PPF:DEF, 3% Irgacure 819, 0.5% Irgacure 784
1:1 PPF:DEF, 3% Irgacure 819, 0.4% Irgacure 784, 0.3% Oxybenzone

## Slide 49
Post cured with no post-processing.
Post cured after post-processing (100% acetone over night).
The Importance of Post Processing Techniques
*Note these SEM images were captured with the scaffold not perfectly aligned.
core area pores are not cleared
core area pores are open
Both of these are the same build with different post-processing handling.
Resin: BY-Full (1:1 PPF:DEF, 3% BAPO, 0.5% I784)

## Slide 50
Notes: 4x increase in resolution
70% reduction in build time
4x increase in strength
Ability to tune strength
Labor and stop free operation
Ability to print more geometries

## Slide 53
{ The Team }
THANK YOU
Notes: Review
Having a robust and commercializable process is essential to bringing a treatment to clinic.
The many variables that can be controlled pose a daunting task to analyze and understand.
We have been able to develop a biodegradable resin that has:
  High resolution,
  Controllable mechanical properties,